## Slide 1: Surface Chemistry
Presented by:
Dr. L. K. Agarwal
Assistant Professor
Department of Chemistry
MohanLal Sukhadia University, Udaipur

## Slide 2: Why Surface ?
Surface of a substance interacts first with its surroundings
Surface molecules are in different state as compared to the molecules in the bulk/interior
Active role in Adsorption, Catalysis, electrodic reactions, chromatography, colloidal formation, Corrosion
Surface chemistry deals with phenomena that occur at interfaces of two surfaces which can be solid-liquid, solid-gas, solid-vacuum, liquid-gas, etc..
Applications:
Catalysis
Colloid Formation
Electrode Reactions
Chromatography

## Slide 3: PRESENTATION FLOW
Surface chemistry
Adsorption : Basics, Principle, Adsorbents Types, commercial Adsobents
Adsorption in Liquidsn & Solids
Adsorbtion Thermodynamics: Spontaneity & Exothermicity
Factors Affecting Adsorption :
Types Of Adsorption
Adsorption Isotherm : Basics & Types , Adsorption Kinetics
Gibbs adsorption isotherm
Estimation of surface area (BET equation),
Surface films on liquids ( Electrokinetic phenomenon)
Catalytic activity at surfaces
Applications of Adsorption

## Slide 4: ADSORPTION : BASICS
A mass transfer process which involves the accumulation of substance at the interface of the two phases, such as, liquid-liquid, gas-liquid
, gas-solid, or liquid-solid interface
OR
Adhesion of atoms, ions, or molecules from a
gas, liquid, or dissolved solid to a surface
ADSORBATE - the substance which is adsorbed on the surface
  ADSORBENT the substance on which surface the adsorbate is adsorbed
  ADSORPTION is a spontaneous process i.e.
ADSORPTION is an exothermic process i.e.
ΔG is negative
ΔH is negative

## Slide 5: TYPES OF ADSORBENTS
Oxygen Containing Compounds
Typically Hydrophilic & Polar
Examples : Silica Gel & Zeolites
Carbon Based Compounds
Typically Hydrophobic & Non Polar Examples : Activated Carbon & Graphite
Polymer Based Compounds
Polar or Non polar functional groups in a porous polymer matrix Examples : Polymers & Resins
Another Classification is based on diameter of pore sizes of Adsorbents
Microporous Adsorbents
Pore Size Range
2 Aº to 20 Aº
Mesoporous Adsorbents
Pore Size Range 20 Aº to 500 Aº
Macroporous Adsorbents
Pore Size Range
> 500 Aº

## Slide 6: COMMERCIAL
ADSORBENTS
Drying of refrigerants , organic solvents, transformer oils
Desiccants in packing & double glazing
Dew Point Control of natural Gas
SILICA GEL
Drying of gases, organic solvents, transformer oils
Removal of HCl from Hydrogen
Removal of fluorine in
Alkylation process
ACTIVATED ALUMINA
Removal of odours from gases
Recovery of solvent vapours
Nitrogen from air
Water purification
Purification of He
ACTIVATED
CARBON
Water Purification
Recovery & purification of steroids & amino acids
Separation of fatty acids from water & toulene
Recovery of proteins & enzymes
POLYMERS & RESINS
Treatment of edible oils
Removal of organic pigments
Refining of mineral oils
Removal of poly chlorinated biphenyls (PCBs)
CLAY
Oxygen from air
Drying of gases
Drying of refrigerants & organic liquids
Pollution control including removal of Hg
Recovery of fructose from Corn Syrup
ZEOLITES

## Slide 7: ADSORPTION : PRINCIPLE
Driving Force for Adsorption
Adsorption is a surface phenomenon and consequence of surface energy
The surface of a liquid or solid is in a state of strain or unsaturation which results in unbalanced residual force at the surface
These unbalanced residual forces results in higher surface energy. Consequently, the surface of liquids/ solids always have a tendency to attract and retain the molecular species with which it comes in contact. This tendency is responsible for the phenomenon of Adsorption
Brunauer, Emmett and Teller's model of multilayer adsorption is a random distribution of molecules on the material surface.

## Slide 8: ADSORPTION IN LIQUIDS & SOLIDS
LIQUID
SOLID
A molecule in the interior of a liquid is,
completely surrounded by other
molecules so, on the average, it is attracted equally in all directions. On a molecule in the surface, however, there is a resultant attraction inwards, because the number of molecules per unit volume is greater in bulk of the liquid than in the vapour, this gives rise to surface tension. Hence, particles at surface and particles at the bulk are in different environment thus giving rise to difference in free energy at the surface & in the bulk.
The Cleavage of a big crystal of solid into smaller units is done to increase
surface area . Due to cleavage of a big crystal into smaller unit, residual forces or vacancies gets generated on the surface of the solid. Occupancy of these vacancies by some other molecular species results into Adsorption
:

## Slide 9: SPONTANEITY & EXOTHERMICITY
For SPONTANEITY ............... at const T & P
As for Spontaneity , ΔG < 0 , hence
ΔH should be negative i.e ΔH < 0
Any process can be represented thermodynamically under constant T & P by
GIBBS EQUATION : ΔG = ΔH – TΔS
ΔG = Gibbs Free Energy , ΔH = Heat of enthalpy , ΔS = Entropy & T = Temperature Adsorption is a SPONTANEOUS process, there is a decrease in the free energy of the system
(ΔG = ΔH – TΔS ). < 0
As translational freedom of adsorbate is reduced when it is adsorbed , thus
ΔS < 0 or negative
ΔG = ΔH – T (-ΔS) ΔG = ΔH + T ΔS
SPONTANEOUS i.e. (ΔG < 0 ) & EXOTHERMIC i.e. ( ΔH < 0 )

## Slide 10: PHYSISORPTION
Physisorption model
Physisorption Model
Molecules and atoms can attach to surface in two ways .
One is Physisorption ( Physical Adsorption ) in which there is a van der Waals interaction between the adsorbate & the substrate. Examples , A dispersion or dipolar- dipolar interaction . Van der Waals interactions are long range but are weak. Energy released when a particle is physisorbed is of the same order of magnitude as the enthalpy of condensation . Such small energies can be absorbed as vibrations of the lattice & dissipated as thermal motion, & a molecule bouncing across the surface will gradually lose all its energy & finally adsorb to it.

## Slide 11: CHEMISORPTIONS
Oxygen molecules - Red adsorbed on metallic surface of Platinum - Purple & Cobalt- Green
Hydrogen atoms - Blue adsorbed on surface of Host - Green & Catalyst - Red
Chemisorption (Chemical Adsorption) in which the molecules or atoms stick to the surface of adsorbent by forming a chemical bond ( usually covalent ),& tend to find sites that maximize their coordination number with the substrate. The distance between the surface & the closest adsorbate atom is also typically shorter for chemisorption . A chemisorbed molecule may be torn apart at the demand of the unsatisfied vacancies of the surface atoms, & the existence of molecular fragments on the surface as a result of chemisorption is one reason why solid surface catalyse reactions .

## Slide 12
PHYSISORPTION / CHEMISORPTION
Physical Adsorption / Physisorption
Not very Specific
No electron transfer , although polarization of
adsorbate may occur
Rapid, non-activated & reversible
No dissociation of adsorbed species
Monolayer or Multilayer
Only significant at relatively low temperatures
Enthalpies are in the region of -20 kJ/mol
As the temperature increases, process
of Physisorption decreases
Chemical Adsorption/Chemisorption
Highly Specific
Electron transfer leading to bond
formation between adsorbate & adsorbent
Activated , may be slow & irreversible
May involve dissociation
Monolayer only
Possible over a wide range of temperatures
Enthalpies are in the region of -200 kJ/mol
With the increases in temperature,
Chemisorption first increases & then decreases

## Slide 13: FACTORS AFFECTING ADSORPTION
Adsorption is an exothermic process. Therefore in accordance with Le Chatelier's principle, the magnitude of adsorption should increases with decrease in temperature. It is in the case of physical adsorption . Chemical adsorption first increases with rise in the temperature and then starts decreasing
TEMPERATURE
PRESSURE
SURFACE AREA
ACTIVATION OF SOLID ADSORBENT
With increase of pressure, adsorption increases up to certain extent till saturation level is achieved - no more adsorption takes place no matter how high the pressure applied.
Activation of adsorbent surface done so as to provide more vacant sites on surface. This can be done by breaking solid crystal in small pieces, breaking lump of solid into powders or sub- dividing the adsorbent
It’s a surface
phenomenon therefore adsorption capacity of
adsorbent increases with increase in its surface area. Smaller the size of particles of solid adsorbents more is the extent of adsorption at its surface interface

## Slide 14: ADSORPTION ISOTHERMS
Adsorption process is usually studied through graphs known as Adsorption Isotherm. The amount of
adsorbate on the adsorbent as a function if its pressure (gas) or concentration (liquid) at constant T
ADSORBATE + ADSORBENT
ADSORPTION
Adsorption
⇌
Desorption
According to Le Chatlier’s principle, on application of excess pressure , the equilibrium will shift
in the direction where number of molecules decreases.
Since no. of molecules decreases in forward direction i.e. direction of Adsorption , with increase of pressure , forward direction equilibrium will be achieved
In the given Adsorption Isotherm , after saturation pressure
Ps adsorption does not increases
Vacancies on the surface of the adsorbent are limited, at Ps a stage is reached when all the sites are occupied and further increase in pressure does not increases adsorption extent. Types of Adsorption Isotherms :
Graph between the amounts of adsorbate (x) adsorbed on the surface of adsorbent (m) and pressure at constant temperature

## Slide 15: FREUNDLICH ISOTHERM
Empirical equation for representing the isothermal variation of adsorption of a quantity of gas
adsorbed by unit mass of solid adsorbent with pressure is Freundlich Adsorption Isotherm
………….
x/m = adsorption per gram of adsorbent which is obtained by dividing the amount of adsorbate (x) by the weight of the adsorbent (m).
P is Pressure, k and n are constants whose values depend upon adsorbent and gas at particular temperature .
Taking the logarithms of Freundlich Isotherm :
Freundlich Isotherm correctly established the relationship of adsorption with pressure at lower values,
Limitation : Failed to predict adsorption capacity at higher pressure
x/m = kP1/n OR x/m = kC1/n
FREUNDLICH ISOTHERM
Log x/m = log k + 1/n log P
Freundlich Isotherm curve
Log x/m versus log P

## Slide 16: LANGMUIR ISOTHERM
.......................
The extent of surface coverage is normally expressed as the fractional coverage, θ
θ = number of adsorption sites occupied / number of adsorption sites available
The rate of change of surface coverage due to adsorption is proportional to the partial pressure p of gas & the number of vacant sites N(1 − θ ), where N is the total number of sites, ka & kd rate constants for adsorption & desorption
dθ/dt = ka pN (1- θ ) ……………………….
The rate of change of θ due to desorption is proportional to the number of adsorbed species, Nθ
dθ/dt = -kd Nθ ..........................
A(g) + M (surface) ⇌ AM(surface)
Rate of Adsorption
In 1916,Langmuir proposed another Isotherm : Langmuir Adsorption isotherm
Based on different assumptions one of which is that dynamic equilibrium exists between adsorbed gaseous molecules and the free gaseous molecule.
A(g) = unadsorbed gaseous
Molecules,
M(surface) = unoccupied adsorbent surface AM(surface ) = Adsorbed gaseous molecules
Rate of Desorption

## Slide 17: CONTINUED.....
At equilibrium there is no net change (that is, the sum of these two rates is zero), and solving for θ
gives the Langmuir Isotherm, where K = (ka / kd)
θ = Kp / ( 1 + Kp)
..............
At lower pressure, Kp is so small that factor (1 + Kp ) in denominator can almost be ignored & Langmuir equation reduces to :
θ = Kp
At higher pressure , Kp is so large that factor ( 1 + Kp) in denominator is nearly equal to Kp &
Langmuir equation reduces to :
θ = Kp / Kp = 1
Limitation
: Valid at low Pressures only and limited to monolayer adsorption
LANGMUIR ISOTHERM
Langmuir isotherm for different values of K

## Slide 18: TEMKIN ISOTHERM
An assumption of the Langmuir isotherm is the independence and equivalence of the adsorption sites.
Deviations from the isotherm can often be traced to the failure of these assumptions
The enthalpy of adsorption often becomes less negative as θ increases, which suggests that the energetically most favourable sites are occupied first.
Temkin Isotherm takes into account all the indirect adsorbate-adsorbate interactions on
adsorption isotherms
θ = c₁ ln (c₂ p)
…………………..
where c1 and c2 are constants, corresponds to supposing that the adsorption enthalpy changes linearly with pressure
TEMKIN
ISOTHERM

## Slide 19: BET ISOTHERM
Most widely used isotherm dealing with multilayer adsorption is BET Isotherm
In physical adsorption , if initial adsorbed layer can act as substrate instead of the isotherm levelling off to some saturated value at high pressures, it can be expected to rise indefinitely
Under the condition of high P & low T , thermal energy of gaseous molecules decreases & more & more gaseous molecules would be available per unit surface area of adsorbent and this leads to multilayer adsorption
BET ISOTHERM
V / Vmon = cz / (1 − z){1 − (1 − c)z} with z = p / p*
p* is the vapour pressure above a layer of adsorbate that is more than one molecule thick & which resembles a pure bulk liquid , Vmon is the monolayer coverage vol., c is a constant
When c >> 1, the BET isotherm takes the simpler form
V / Vmon = 1 / (1 – z )
BET Isotherm for different values of c

## Slide 20: ADSORPTION KINETIC MODELS
substances from
aq. solns
pseudo- first-order rate constant
for the kinetic model
Pseudo Second Order Rate Equation
A Pseudo second order rate equation proposed is :
(HP)0 equilibrium sites available on Peat, (HP)t equilibrium sites
available on Peat at time t , kp2 pseudo second order rate constant for kinetic Model.
Used in adsorption of metal ions, dyes, herbicides, oils, & organic
Adsorption reaction models developed to describe Adsorption Kinetics
Pseudo First Order Rate Equation
A first-order rate equation to describe the kinetic process of liquid-solid phase adsorption of oxalic acid and malonic acid onto charcoal
Mostly used in adsorption of pollutants from wastewater in different fields
qe & qt (mg/g) Ads. cap,. at eqm & time t (min), resp. kp1 (min−1) is the
dqt / dt = kp1 ( qe – qt )
t
d (P) / dt = k
p2
[ (P)0 - (P)t ]2

## Slide 21: CONTINUED ......
The typical second-order rate equation in solution systems is.
Ct (mg/L) is the concentration of solute at time t (min), respectively, &
k2 (L/(mg·min)) is the rate constant.
Used to describe fluoride adsorption onto acid-treated spent bleaching
earth & phosphamidon adsorption on an antimony(V) phosphate cation
exchanger
aq. solns
Second Order Rate Equation
Elovich’ s Equation
A kinetic equation of chemisorptions was established Elovich’s Eq
q represents the amount of gas adsorbed at time t, a the desorption constant, and α the initial adsorption rate.
Widely used to describe the adsorption of gas onto solid systems & adsorption process of pollutants from
dq /dt = ae-αq
dCt / dt = -k2Ct2

## Slide 22: APPLICATIONS OF ADSORPTION
Separation and purification of liquid and gas mixtures, bulk chemicals, isomers and air
Drying gases and liquids before loading them in industrial
systems
Removal of impurities from liquid and gas media
Recovery of chemicals from industrial and vent gases &

Water Purification

## Slide 23: REFERENCES
Physical Chemistry , 9th edition by Peter Atkins
Physical chemistry , 2nd edition by Samuel Glasstone
Treatment of Waste water with Low cost adsorbent – A review ; Vol 4 ;
VSRD International Journals ; Uttam Singh & Rajesh Kumar Kansal
Adsorption – Wikipedia
Adsorption – from theory to Practice ; Journal of Advances in colloid & interface sciences ; A. Dabrowski
Critical review in adsorption kinetic models; Journal of Zhejiang University Science A ; Hui Qiu, Lu yv, Bing-cai Pan, Qing-jian Zhang, Wei-ming Zhang,
Quan-xing Zhang
Chemistry Learning – Adsorption
Its all about chemical engineering – Blogspot
My chemistry works – Blogspot
Adsorption by Piero M. Armentate NJIT
Factors affecting Adsorption – Sciencehq
Separation Process – Adsorption – Chapter 1
Adsorption Isotherm – Physical Chemistry virtual lab